PRODUCT: ECOSOFT 306

Highly effective non-yellowing, economical micro amino silicone for permanent finish

effects on all types of fibers.

- Confers a pleasant, soft, slightly bulky handle on the goods.

- Improves sew ability.

- As an additive in synthetic resin finishes improve the technological properties of the

- goods. (Creasing behavior, tensile strength)

- Applied by the padding method.

- Improves the stretch and recovery capacity of knit goods.

- Produces finish effect that are fast to washing and dry cleaning.

- Also suitable for finishing articles made of open-end (OE) yarns.

PROPERTIES

Appearance                                                       :  Pale yellowish / water white Liquid.

Chemical Character                                           : Modified poly-siloxane.

Ionic Character                                                  : Nonionic.

APPLICATION

1 Padding on all type of fibers

Ecosoft  306 Liq                                                 Doses  : 5 to 20 g/l

Acetic acid to maintain PH 5 to 5.5    Tem <40°C

Pad(pick up 65-85%) – Dry at 120-130°C

2  By Exhaustion on all type of fibers

Ecosoft  306 Liq                                                 Doses  : 1-3% owm

Acetic acid to maintain PH 5 to 5.5    Tem <40°C

Time 20-25 Mins    -    Dry at 120-130°C

REMARK

- As with all silicone emulsions, care should be taken to ensure adequate rinsing to remove chemical residues after pre-treatment or dyeing. Care also should be taken to avoid alkalinity of goods, high temperature both on fabrics & in the bath as this can lead to spots.

- It is advisable to store silicon emulsions in cool place, around 25°C with a tightly closed lid.

- Shelf life of the product is 6 months when stored in specified conditions. Storage beyond shelf life does not mean that product is not usable but it is advisable to check the properties of the product for intended use for quality assurance purpose.

Company warrants that its products will confirm to company specification. Company’s liability is limited to the refund of purchase price, or replacement of product. Company will not be responsible for incidental or consequential damages of any kind. It is the user’s responsibility to determine the suitability of use.