PRODUCT:  Eco soft CWS (LOW YELLOWING COLD WATER SOLUBLE)

Uses:

- Softening woven and knitted fabrics by pad or exhaust application.

- Additive for resin finishes

Technical Data:

- Is easily soluble in cold water at room temperature, so ease in handling & dissolution.

- Imparts excellent surface softness for all types of fibers.

- Is suitable for woven and knitted fabric.

- Good elasticity

- Good lubricating effect.

- Antistatic effect.

Properties:

| Ionic Nature | : | Cationic |
| --- | --- | --- |
| Physical Aspect | : | Creamish Flakes |
| Solubility | : | In cold water easily |
| Nature | : | Low yellowing |

Application:

Dissolving / Diluting

Dissolve readily in cold water by slow speed stirring. Dissolution could be accelerated by raising the temperature. Viscosity of the dissolved product increases as temperature increases. It is recommended to filter the solution before the application to remove any undissolved particles.

Cationic Softener 100% is recommended to be dissolved 1 to 10, but this may be reduces to a maximum of 1 to 5.

APPLICATION DATA ON THE DILUTED PRODUCT:

Special Advantages

- Minimizes scoring of bleached cotton during heat setting.

- Substantive to textile fibers therefore economically applicable from long liquors

- Imparts ideal frictional properties to fiber for many conversion processes

Application Methods:

Being cationic Softener 100% paste will have affinity for fibers and can therefore be applied by exhaust methods. A pH of 6.00 to 7.0 is therefore be applied by exhaust methods. A pH of 6.00 to 7.0 is recommended for maximum exhaustion. It is also applicable by pad or immersion / squeeze technique, the bath being continuously recharged during the process.

Pad Application:

1-3 g/l 100 %( 10% diluted emulsion

10 – 30 g/l 100 %( 10% diluted emulsion)

Exhaust Application:

0.1-0.3 g/l 100% (10% diluted emulsion

1 – 3 g/l 100% (10% diluted emulsion)